                                                                                          
[image: image1]
TECHNICAL INFORMATIONS – POWDER COATINGS

[image: image1][image: image2.png]


[image: image3.jpg]




POLITHERM 26 R SM WHITE 64982 BR  
	
	

	PRODUCT:
	15531584

	DESCRIPTION / USES:

	Metallic parts coating for outdoor use.

	CHARACTERISTICS:

	
	Resin:
	 Polyester

	
	Specific gravity:
	1,72 ± 0,10 g/cm3

	
	Stability:
	12 month (max. 30ºC)

	
	Observations:
	Free of heavy metals and other substances provided for in Directive 2015/863 EU of 03/31/2015 (RoHS).

	APPLICATION CHARACTERISTICS:

	
	
	

	
	Surface:
	Ferrous and non-ferrous

	
	Surface preparation:
	Ferrous : Phosphatization

	
	
	Non-ferrous: Chromatization or phosphatization*

	
	Cure conditions:
	10 minutes at 200 ºC**

	
	Thickness:
	60 – 80 µm

	
	Application system:
	Electrostatic gun

	
	

	AFTER CURE CHARACTERISTICS:***

	
	TEST
	METHOD
	SPECIFICATION

	
	ADHESION
	WPS-3905
	: GR0

	
	GLOSS @ 60°
	WPS-3854
	: Min 85 UB   

	
	IMPACT (REVERSE)
	WPS-4130
	: Min 50 kg X cm

	
	FLEXIBILITY (CONIC MANDREL)
	WPS-4856
	: Max 3 mm

	
	

	CHEMICAL RESISTANCE ***

	
	Salt spray:
	: Min. 500 h (ASTM B117 – 03)

	
	Humidity:
	: Min. 1000 h (35ºC)

	

	* For non-ferrous metals phosphatizing, please contact our technical service.

**   After stabilization on correct temperature (metal temperature).

*** The tests were conducted on degreased steel panels in accordance with the cure and thickness specifications.  The results may vary, depending on the surface characteristics. For chemical resistance testing, panels were degreased and treated with tricationic phosphat.

IMPORTANT: This coating, when properly applied and cured is suitable for the use of adhesives and sealants. However, because of the different products on the market, it requires prior testing by the user in order to select the adhesive and / or sealant appropriate.
If is not possible the use of the product according to the directions given above we ask you to contact our technical service.

STORAGE: Fresh, dry and covered place.





Review: 00                                                                                                                                                                            Date: 26/06/20

